TOWN OF CHESTER

INVITATION TO BID

WINTER SAND

The Town of Chester is accepting bids for up to 5,000 cubic yards of winter sand.  The material shall meet or exceed State of Vermont/ASHTO specifications.  The Town is seeking loaded pit price:

SPECIFICATION FOR WINTER SAND

1.   The winter sand shall be clean, screened, uniformly graded from coarse to fine and free from silt, loam, clay and of organic matter.  The sand shall meet or exceed the following requirements:

Sieve designation % by weight passing square mess sieve

Up to  		9/16		100

No		4		90-100

No		100		2-10

2.   The materials will be sampled and tested by the Chester Highway Foreman.  The town reserves the right to test product at any time during this process.

3.   The winter sand will be picked up and hauled by the Town of Chester Highway Department.  There will be no delivery required.  All material must be available so that this can be completed by November 19, 2016.

The Town of Chester reserves the right to accept or reject any and all bids.

All bids must be received at the Chester Town Office no later than 3:00 p.m. on Wednesday, October 12, 2016.

TOWN OF CHESTER

WINTER SAND

BID FORM

Sieve designation % by weight passing square mess sieve

Up to 9/16		_______________________________

No 4			_______________________________

No 100			_______________________________

Price per cubic yard	$_______________________________

All sand to be received in the town pit by November 14, 2016.